## Slide 1
Non-Volatile Memories issues in space radiative environment
November 19th 2025

## Slide 2
BITFLIP
Impact des fautes
19 nov. 2028
16h20-16h40
Réfectoire
Non-Volatile Memories issues in space radiative environment
Guillaume Bourg-Cazan
Radiation test Manager at Microchip

## Slide 3: Introduction
Aging
Single Event Effects
Write in flight
Possible Mitigations
Conclusion

## Slide 4: Types of failures
Aging
  TID (Total Ionizing Dose)
Single Event Effects
  Memory corruption
  Single bit flip
  Write in flight

## Slide 5: Aging

## Slide 6
TID -Total Ionizing Dose
Reminder of the observed effects
Vcell
Dose
Read reference
Vcell
Dose
margin
Read reference
Dose is a cumulated effect (ex: 1krad(Si)/year at ISS level)
Effect on the device throughout its lifetime
The key point is the difference between the cellule voltage (Vcell) and the reference voltage called margin
Data retention
    Vcell vs Dose
Degradation of reading references
    When the refence move, the margin between the reference and Vcell change
    If the margin is too low, the read is not reliable or fail
Write
Read
Reference
“1” or “0”
Data In
“1” or “0”
Vcell
HV

## Slide 7: Total Ionizing Dose (TID)
Destructive test
  Prior to the irradiation, all units are programmed and measured
  Irradiation performed on Co60 source
  Dedicated board
  Static mode
Periodic readout during exposure
  Measure of critical parameters on ATE
Annealing
  Measure of critical parameters ATE
Testing

## Slide 8: Total Ionizing Dose (TID)
Results
1 krad/y
5 krad/y
15 krad/y
10 krad/y
Microchip Device | TID in krad (Si)
SST26LF064RT | 30
SST38LF6401RT | 50
SAMV71RT | 30 (read only) 25 (write)

## Slide 9: Single Event Effects

## Slide 10: Single Effect Events
Unexpected Write
The embedded controller could perform write due to Heavy particles impact
Test method
  Dedicated test on particle accelerator
  Very specific test environment (tester, board, device preparation, …)
Controller
Wrapper
HV
Particule

## Slide 11: Single Effect Events
Bit flip
Due to heavy particle strike, charge trapped in floating gate can be affected
A single bit can flip even on an unbiased device
Test method
  Dedicated test on particle accelerator
  Very specific test environment (tester, board, device preparation, …)
p- substrate
Floating gate
n+
n+
Drain
Oxide
- - - - - - - - - - - -
Source
- - - - - - - - - - - - -
+ + + + + + + + + + +
Control gate
Particle
VGS
ID
After
Before
Read reference

## Slide 12: Write in Flight

## Slide 13: Write in Flight
TID
High voltage into the device to perform Erase/Programing operations
  TID reduces the charge pump capability
  TID increase the array leakage and overstress programing circuitry
Consequences
  Bad Erase and/or Programming : The device in no more usable
  Data retention issue
Write
Read
Reference
“1” or “0”
Data In
“1” or “0”
Vcell
HV
Vcell
Dose
The charge pump becomes too weak
ref

## Slide 14: Write in Flight
Destructive effect
High voltage into the device to perform Erase/Programing operations
  If a heavy ion strike the device in a high voltage regions this can lead to a SEGR (Single Event Gate Rupture)
Test method
  Dedicated test on particle accelerator
  Very specific test environment (tester, board, device preparation, …)
p- substrate
Floating gate
n+
n+
Drain
Oxide
- - - - - - - - - - - -
Source
- - - - - - - - - - - - -
+ + + + + + + + + + +
Control gate
Particle
- - - - - - - - - - - - -
Gate rupture
Before Irrad.
After Irrad.
VDS = 0.1V; Krypton 1259 MeV
Ref. NSREC paper
D. Truyen et al, "Single Event Dielectric Rupture Characterization of Microchip High Voltage Devices," 2019 IEEE Radiation Effects Data Workshop, San Antonio, TX, USA, 2019, pp. 1-8, doi: 10.1109/REDW.2019.8906623.

## Slide 15: Single Effect Events
Results
Microchip Devices | Bit flip MTBF (ISS LEO)
SST26LF064RT | 2.28E10 days 62E6 years
SST38LF6401RT | 13.4E3 days 38 years
SAMV71RT | 15E6 days 41E3 years
SAMRH71* | None
* : RHBD device (Radiation Hardened by Design)

## Slide 16: Possible Mitigations

## Slide 17: Mitigations
TID
Process
  Reduce oxide thickness
  Adding Implants to modify the parasitic transistor parameters
Design
  Choose the best technology node
  Use proven blocs
  Oversize charge pump
  Enclosed Layout transistor
Mass production (Yield impact)
  Configure the device in the better manner
    Vref configuration to anticipate drift
    Properly use spare mechanism
  Unit screening
    reject worst devices ( Margin )
Application
  Re-program the device periodically
  Shielding
Radiation induced degradation in STI oxides
+++++
+++++
Pwell / Sub
Poly. Gate
Oxides (STI)
Oxide-trapped charge charge build up in STI
Drain-source leakage path in NMOS
Mitigation
Enclosed Layout Transistor (ELT)
No radiation-induced conducting path between source and drain
G
D
S
Linear transistor
Ioff
Ioff
Enclosed Layout transistor
Enhancement of the leakage

## Slide 18: Mitigations
Design
  ECC (Error Correction Code) improves the single bit flip reluctance
  Redundancy control logic
    Dice (Dual Interlocked Cell)
    TMR (Triple Modular Redundancy)
Application
  Lock the device to prevent unexpected write operations
  Duplicate the code in several regions of the memory and perform a sanity check periodically
Single Effects
TMR: Triple Modular Redundancy
DICE: Dual-Interlocked Cell memory Pass-gates are not shown
Intrinsically immune to single node particle hit

## Slide 19: Conclusion
Non-Volatile Memories are not “simple” digital bloc
High variability depending on the technology (process)
TID affect the lifetime
SEE can affect suddenly the device (SEGR, BitFlip, SEU)
The application can improve the behavior using suitable guides lines

## Slide 20: Thank you for your attention
Questions?